## Slide 1: U.S. UPLAND COTTON QUALITY
2022-23 CROP
Final

## Slide 2
YIELD TREND U.S. UPLAND
POUNDS/ACRE
YEAR

## Slide 3: MICRONAIRE

## Slide 4: MICRONAIRE TREND U.S. UPLAND
MICRONAIRE
YEAR
Chart: 
| 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
 | 4.3948 | 4.4808 | 4.4163 | 4.428 | 4.0534 | 4.3922 | 4.4726 | 4.2678 | 4.1484 | 4.3372

## Slide 5: MICRONAIRE DISTRIBUTION U.S. UPLAND
MICRONAIRE
PERCENT OF SAMPLES

## Slide 6: AVERAGE MICRONAIRE
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2020 | 4.2523 | 4.4472 | 4.5137 | 4.388 | 4.5871 | 4.3195 | 3.9156 | 3.7694 | 4.0721 | 4.4616
2021 | 4.3692 | 4.2922 | 4.5546 | 4.3108 | 4.5717 | 4.4181 | 3.94 | 3.7497 | 3.8558 | 4.3104
2022 | 4.4642 | 4.288 | 4.7342 | 4.3685 | 4.6972 | 4.3802 | 4.0044 | 3.8929 | 4.1126 | 4.4376
CLASSING OFFICE
MICRONAIRE

## Slide 7: AVERAGE MICRONAIRE
MICRONAIRE
LOCATION
Far West
Southwest
Mid South
Southeast
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2020 | 4.2899 | 4.4171 | 4.4634 | 4.2866 | 4.2396 | 4.237 | 4.4633 | 4.6332 | 4.558 | 4.3618 | 4.3045 | 4.3195 | 3.9156 | 3.7694 | 4.0721 | 4.0432 | 3.2988 | 4.2613 | 4.5715 | 4.2592
2021 | 4.4399 | 4.1505 | 4.2936 | 4.2839 | 4.4169 | 4.3268 | 4.3107 | 4.5263 | 4.6245 | 4.4346 | 4.3086 | 4.4181 | 3.94 | 3.7497 | 3.8548 | 3.8651 | 4.2464 | 3.8333 | 4.3094 | 4.4202
2022 | 4.2732 | 4.2512 | 4.3059 | 4.3801 | 4.5289 | 4.314 | 4.3526 | 4.6484 | 4.7845 | 4.4763 | 4.3076 | 4.3802 | 4.0044 | 3.8929 | 4.1126 | 3.9208 | 3.9893 | 3.9113 | 4.514 | 4.4027

## Slide 8: STRENGTH

## Slide 9: STRENGTH TREND U.S. UPLAND
GRAMS/TEX
YEAR
Chart: 
| 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
 | 30.2238 | 30.0579 | 30.3444 | 30.339 | 29.9075 | 29.9014 | 30.6086 | 30.6073 | 30.6304 | 30.6653

## Slide 10: STRENGTH DISTRIBUTION U.S. UPLAND
GRAMS/TEX
PERCENT OF SAMPLES

## Slide 11: AVERAGE STRENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2020 | 29.9431 | 29.9226 | 31.3938 | 31.0616 | 30.885 | 30.8824 | 30.651 | 30.3982 | 30.2969 | 31.9502
2021 | 30.6924 | 29.9804 | 31.1306 | 31.0581 | 31.303 | 30.8702 | 30.5799 | 30.481 | 30.2283 | 32.2439
2022 | 30.8763 | 30.3265 | 30.8444 | 30.537 | 31.3212 | 29.8005 | 31.2465 | 31.0134 | 30.7026 | 32.12
CLASSING OFFICE
GRAMS/TEX

## Slide 12: AVERAGE STRENGTH
GRAMS/TEX
LOCATION
Far West
Southwest
Mid South
Southeast
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2020 | 30.2173 | 30.2719 | 29.8333 | 29.6554 | 30.1255 | 29.7212 | 30.6277 | 30.9529 | 31.6114 | 31.2533 | 31.2192 | 30.8824 | 30.651 | 30.3982 | 30.2969 | 31.148 | 29.5278 | 30.1427 | 31.6451 | 33.1215
2021 | 31.0603 | 30.4956 | 29.8325 | 30.2377 | 30.9474 | 30.465 | 30.8439 | 31.2271 | 31.279 | 31.3419 | 30.9533 | 30.8702 | 30.5799 | 30.481 | 30.2283 | 31.305 | 30.9734 | 30.398 | 31.9033 | 33.8795
2022 | 31.0228 | 30.6722 | 30.2385 | 30.4746 | 31.0527 | 30.8409 | 30.4465 | 31.0668 | 30.9901 | 30.8294 | 30.4373 | 29.8005 | 31.2465 | 31.0134 | 30.7026 | 31.8419 | 30.625 | 30.9379 | 32.0033 | 32.9979

## Slide 13: LENGTH

## Slide 14: LENGTH TREND U.S. UPLAND
32’s OF AN INCH
YEAR
Chart: 
| 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
 | 35.8506 | 35.6512 | 35.8955 | 36.2879 | 36.4464 | 36.5288 | 36.4708 | 37.0888 | 36.6557 | 36.9118

## Slide 15: LENGTH DISTRIBUTION U.S. UPLAND
PERCENT OF SAMPLES
32’S OF AN INCH

## Slide 16: AVERAGE LENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2020 | 37.5337 | 37.0632 | 38.1446 | 38.0697 | 38.3969 | 36.5824 | 36.2288 | 35.7633 | 35.1055 | 37.2076
2021 | 36.6973 | 36.6714 | 37.9285 | 37.7066 | 38.1514 | 36.8531 | 35.8178 | 35.8608 | 35.3442 | 37.5606
2022 | 36.9933 | 36.4858 | 37.0124 | 37.4332 | 37.9774 | 35.2443 | 36.6702 | 36.7602 | 36.4243 | 37.4387
CLASSING OFFICE
32’S OF AN INCH

## Slide 17: AVERAGE LENGTH
32’S OF AN INCH
LOCATION
Far West
Southwest
Mid South
Southeast
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2020 | 37.6472 | 37.3196 | 37.0221 | 37.5257 | 37.4158 | 38.091 | 37.3545 | 38.2687 | 38.5824 | 38.4899 | 38.381 | 36.5824 | 36.2288 | 35.7633 | 35.1055 | 36.9726 | 35.2281 | 36.7763 | 37.0704 | 37.6
2021 | 37.7013 | 37.2166 | 36.599 | 36.954 | 36.5563 | 36.8111 | 37.409 | 38.1288 | 38.2679 | 37.8237 | 37.7379 | 36.8531 | 35.8178 | 35.8608 | 35.3442 | 36.8049 | 35.1577 | 37.3573 | 37.5748 | 37.5767
2022 | 36.4474 | 36.8283 | 36.4899 | 37.3145 | 36.8714 | 36.9231 | 37.4764 | 37.7185 | 37.1663 | 37.5617 | 37.5322 | 35.2443 | 36.6702 | 36.7602 | 36.4243 | 37.3176 | 35.0852 | 37.7087 | 37.4845 | 37.1332

## Slide 18: LENGTH UNIFORMITY INDEX

## Slide 19: LUI TREND U.S. UPLAND
LUI PERCENT
YEAR

## Slide 20: LENGTH UNIFORMITY DISTRIBUTION U.S. UPLAND
LUI PERCENT
PERCENT OF SAMPLES

## Slide 21: AVERAGE LENGTH UNIFORMITY
CLASSING OFFICE
LUI PERCENT

## Slide 22: AVERAGE LENGTH UNIFORMITY
LUI PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2020 | 81.2428 | 81.2686 | 81.3984 | 81.2029 | 81.5421 | 81.8046 | 81.8545 | 81.6433 | 82.0839 | 81.9346 | 82.2449 | 81.2157 | 80.2844 | 80.247 | 79.7801 | 80.6432 | 79.8232 | 81.105 | 81.0901 | 81.5605
2021 | 81.8134 | 81.3638 | 81.0595 | 81.3069 | 81.924 | 82.0568 | 82.1801 | 82.1241 | 82.4075 | 82.2081 | 82.0578 | 81.49 | 80.254 | 80.1074 | 79.6824 | 80.6139 | 80.761 | 81.033 | 81.0734 | 81.8478
2022 | 81.4756 | 81.3645 | 81.2161 | 81.6839 | 82.2328 | 82.334 | 81.8234 | 82.175 | 81.6341 | 82.0071 | 81.6982 | 80.8782 | 80.4435 | 80.5581 | 80.4286 | 80.7263 | 80.097 | 80.9983 | 81.2 | 81.3415

## Slide 23: COLOR & LEAF

## Slide 24: COLOR GRADE TREND U.S. UPLAND
YEAR
PERCENT COLOR GRADE

## Slide 25: COLOR GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES

## Slide 26: PERCENT WHITE GRADES
CLASSING OFFICE
PERCENT

## Slide 27: PERCENT WHITE GRADES
PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2020 | 91.2221 | 89.1388 | 89.0266 | 94.0844 | 94.6281 | 96.3533 | 98.247 | 96.8114 | 91.4729 | 98.9305 | 99.358 | 84.3697 | 81.0551 | 86.9178 | 85.4841 | 83.6544 | 70.2175 | 99.0125 | 98.2362 | 98.7223
2021 | 93.6821 | 96.6713 | 94.0621 | 97.8215 | 99.0754 | 99.6697 | 99.3808 | 98.3784 | 98.3799 | 98.6868 | 98.992 | 93.4521 | 92.4845 | 92.1157 | 95.643 | 94.0618 | 94.9324 | 99.9704 | 96.8947 | 95.9012
2022 | 98.1161 | 97.3053 | 98.0113 | 97.8626 | 97.3677 | 99.1345 | 94.5881 | 98.1398 | 90.474 | 99.2014 | 99.4466 | 78.5443 | 87.4032 | 93.6313 | 94.0612 | 91.3393 | 80.5839 | 95.881 | 96.8995 | 97.0155

## Slide 28: LEAF GRADE DISTRIBUTION U.S. UPLAND
LEAF GRADE CODE
PERCENT OF SAMPLES

## Slide 29: COLOR & LEAF GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES

## Slide 30: INFORMATION ON THE WEB
https://www.cottoninc.com/cotton-production/quality/cotton-crop-quality/