## Slide 1: U.S. UPLAND COTTON QUALITY
2023-24 CROP
Final
Fiber Competition, Cotton Incorporated

## Slide 2
YIELD TREND U.S. UPLAND
POUNDS/ACRE
YEAR
Fiber Competition, Cotton Incorporated

## Slide 3: MICRONAIRE
Fiber Competition, Cotton Incorporated

## Slide 4: MICRONAIRE TREND U.S. UPLAND
MICRONAIRE
YEAR
Fiber Competition, Cotton Incorporated
Chart: 
| 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023
 | 4.4808 | 4.4163 | 4.428 | 4.0534 | 4.3922 | 4.4726 | 4.2678 | 4.1484 | 4.3372 | 4.5221

## Slide 5: MICRONAIRE DISTRIBUTION U.S. UPLAND
MICRONAIRE
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 6: AVERAGE MICRONAIRE
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2021 | 4.3692 | 4.2922 | 4.5546 | 4.3108 | 4.5717 | 4.4181 | 3.94 | 3.7497 | 3.8558 | 4.3104
2022 | 4.4642 | 4.288 | 4.7342 | 4.3685 | 4.6972 | 4.3802 | 4.0044 | 3.8929 | 4.1126 | 4.4376
2023 | 4.659 | 4.4463 | 4.6835 | 4.5323 | 4.8579 | 4.3415 | 4.1981 | 4.5015 | 4.5271 | 4.3636
CLASSING OFFICE
MICRONAIRE
Fiber Competition, Cotton Incorporated

## Slide 7: AVERAGE MICRONAIRE
MICRONAIRE
LOCATION
Far West
Southwest
Mid South
Southeast
Fiber Competition, Cotton Incorporated
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2021 | 4.4399 | 4.1505 | 4.2936 | 4.2839 | 4.4169 | 4.3268 | 4.3107 | 4.5263 | 4.6245 | 4.4346 | 4.3086 | 4.4181 | 3.94 | 3.7497 | 3.8548 | 3.8651 | 4.2464 | 3.8333 | 4.3094 | 4.4202
2022 | 4.2732 | 4.2512 | 4.3059 | 4.3801 | 4.5289 | 4.314 | 4.3526 | 4.6484 | 4.7845 | 4.4763 | 4.3076 | 4.3802 | 4.0044 | 3.8929 | 4.1126 | 3.9208 | 3.9893 | 3.9113 | 4.514 | 4.4027
2023 | 4.7146 | 4.4125 | 4.4198 | 4.4688 | 4.7775 | 4.519 | 4.341 | 4.8315 | 4.7605 | 4.7022 | 4.5651 | 4.3415 | 4.1981 | 4.5015 | 4.5271 | 4.2874 | 3.7499 | 4.4297 | 4.358 | 4.2983

## Slide 8: STRENGTH
Fiber Competition, Cotton Incorporated

## Slide 9: STRENGTH TREND U.S. UPLAND
GRAMS/TEX
YEAR
Fiber Competition, Cotton Incorporated
Chart: 
| 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023
 | 30.0579 | 30.3444 | 30.339 | 29.9075 | 29.9014 | 30.6086 | 30.6073 | 30.6304 | 30.6653 | 30.84

## Slide 10: STRENGTH DISTRIBUTION U.S. UPLAND
GRAMS/TEX
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 11: AVERAGE STRENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2021 | 30.6924 | 29.9804 | 31.1306 | 31.0581 | 31.303 | 30.8702 | 30.5799 | 30.481 | 30.2283 | 32.2439
2022 | 30.8763 | 30.3265 | 30.8444 | 30.537 | 31.3212 | 29.8005 | 31.2465 | 31.0134 | 30.7026 | 32.12
2023 | 30.8865 | 30.892 | 30.9876 | 30.466 | 31.3263 | 30.3657 | 31.5871 | 31.0469 | 30.6525 | 32.4153
CLASSING OFFICE
GRAMS/TEX
Fiber Competition, Cotton Incorporated

## Slide 12: AVERAGE STRENGTH
GRAMS/TEX
LOCATION
Far West
Southwest
Mid South
Southeast
Fiber Competition, Cotton Incorporated
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2021 | 31.0603 | 30.4956 | 29.8325 | 30.2377 | 30.9474 | 30.465 | 30.8439 | 31.2271 | 31.279 | 31.3419 | 30.9533 | 30.8702 | 30.5799 | 30.481 | 30.2283 | 31.305 | 30.9734 | 30.398 | 31.9033 | 33.8795
2022 | 31.0228 | 30.6722 | 30.2385 | 30.4746 | 31.0527 | 30.8409 | 30.4465 | 31.0668 | 30.9901 | 30.8294 | 30.4373 | 29.8005 | 31.2465 | 31.0134 | 30.7026 | 31.8419 | 30.625 | 30.9379 | 32.0033 | 32.9979
2023 | 32.2471 | 30.9694 | 30.7718 | 30.9111 | 31.0875 | 30.031 | 30.2302 | 31.1703 | 31.2221 | 30.7671 | 30.3724 | 30.3657 | 31.5871 | 31.0469 | 30.6525 | 31.7573 | 31.7139 | 31.3091 | 32.2897 | 33.2995

## Slide 13: LENGTH
Fiber Competition, Cotton Incorporated

## Slide 14: LENGTH TREND U.S. UPLAND
32’s OF AN INCH
YEAR
Fiber Competition, Cotton Incorporated
Chart: 
| 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023
 | 35.6512 | 35.8955 | 36.2879 | 36.4464 | 36.5288 | 36.4708 | 37.0888 | 36.6557 | 36.9118 | 36.374

## Slide 15: LENGTH DISTRIBUTION U.S. UPLAND
PERCENT OF SAMPLES
32’S OF AN INCH

## Slide 16: AVERAGE LENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2021 | 36.6973 | 36.6714 | 37.9285 | 37.7066 | 38.1514 | 36.8531 | 35.8178 | 35.8608 | 35.3442 | 37.5606
2022 | 36.9933 | 36.4858 | 37.0124 | 37.4332 | 37.9774 | 35.2443 | 36.6702 | 36.7602 | 36.4243 | 37.4387
2023 | 35.9804 | 36.1888 | 36.2471 | 36.9969 | 36.7048 | 35.3088 | 36.2374 | 35.7335 | 35.4389 | 37.3935
CLASSING OFFICE
32’S OF AN INCH
Fiber Competition, Cotton Incorporated

## Slide 17: AVERAGE LENGTH
32’S OF AN INCH
LOCATION
Far West
Southwest
Mid South
Southeast
Fiber Competition, Cotton Incorporated
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2021 | 1.1782 | 1.163 | 1.1437 | 1.1548 | 1.1424 | 1.1503 | 1.169 | 1.1915 | 1.1959 | 1.182 | 1.1793 | 1.1517 | 1.1193 | 1.1207 | 1.1045 | 1.1502 | 1.0987 | 1.1674 | 1.1742 | 1.1743
2022 | 1.139 | 1.1509 | 1.1403 | 1.1661 | 1.1522 | 1.1538 | 1.1711 | 1.1787 | 1.1614 | 1.1738 | 1.1729 | 1.1014 | 1.1459 | 1.1488 | 1.1383 | 1.1662 | 1.0964 | 1.1784 | 1.1714 | 1.1604
2023 | 1.125 | 1.1369 | 1.1326 | 1.1413 | 1.1177 | 1.1214 | 1.1574 | 1.1422 | 1.1379 | 1.1527 | 1.1632 | 1.1034 | 1.1324 | 1.1167 | 1.1075 | 1.1342 | 1.1177 | 1.1694 | 1.17 | 1.1713

## Slide 18: LENGTH UNIFORMITY INDEX
Fiber Competition, Cotton Incorporated

## Slide 19: LUI TREND U.S. UPLAND
LUI PERCENT
YEAR
Fiber Competition, Cotton Incorporated

## Slide 20: LENGTH UNIFORMITY DISTRIBUTION U.S. UPLAND
LUI PERCENT
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 21: AVERAGE LENGTH UNIFORMITY
CLASSING OFFICE
LUI PERCENT
Fiber Competition, Cotton Incorporated

## Slide 22: AVERAGE LENGTH UNIFORMITY
LUI PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION
Fiber Competition, Cotton Incorporated
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2021 | 81.8134 | 81.3638 | 81.0595 | 81.3069 | 81.924 | 82.0568 | 82.1801 | 82.1241 | 82.4075 | 82.2081 | 82.0578 | 81.49 | 80.254 | 80.1074 | 79.6824 | 80.6139 | 80.761 | 81.033 | 81.0734 | 81.8478
2022 | 81.4756 | 81.3645 | 81.2161 | 81.6839 | 82.2328 | 82.334 | 81.8234 | 82.175 | 81.6341 | 82.0071 | 81.6982 | 80.8782 | 80.4435 | 80.5581 | 80.4286 | 80.7263 | 80.097 | 80.9983 | 81.2 | 81.3415
2023 | 81.787 | 81.7365 | 81.4101 | 81.8823 | 82.0729 | 81.9659 | 82.3 | 82.3694 | 82.0275 | 82.4526 | 82.3576 | 81.0662 | 80.5488 | 80.4131 | 80.2823 | 80.8799 | 79.9374 | 81.5561 | 81.5268 | 82.0013

## Slide 23: COLOR & LEAF
Fiber Competition, Cotton Incorporated

## Slide 24: COLOR GRADE TREND U.S. UPLAND
YEAR
PERCENT COLOR GRADE
Fiber Competition, Cotton Incorporated

## Slide 25: COLOR GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 26: PERCENT WHITE GRADES
CLASSING OFFICE
PERCENT
Fiber Competition, Cotton Incorporated

## Slide 27: PERCENT WHITE GRADES
PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION
Fiber Competition, Cotton Incorporated
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2021 | 93.6821 | 96.6713 | 94.0621 | 97.8215 | 99.0754 | 99.6697 | 99.3808 | 98.3784 | 98.3799 | 98.6868 | 98.992 | 93.4521 | 92.4845 | 92.1157 | 95.643 | 94.0618 | 94.9324 | 99.9704 | 96.8947 | 95.9012
2022 | 98.1161 | 97.3053 | 98.0113 | 97.8626 | 97.3677 | 99.1345 | 94.5881 | 98.1398 | 90.474 | 99.2014 | 99.4466 | 78.5443 | 87.4032 | 93.6313 | 94.0612 | 91.3393 | 80.5839 | 95.881 | 96.8995 | 97.0155
2023 | 89.1098 | 96.8864 | 96.6194 | 98.5495 | 99.0693 | 99.4865 | 99.7966 | 98.1944 | 85.7296 | 99.5762 | 99.8996 | 63.5594 | 76.0182 | 84.3183 | 81.8777 | 79.0539 | 66.3027 | 97.3877 | 98.8416 | 98.3345

## Slide 28: LEAF GRADE DISTRIBUTION U.S. UPLAND
LEAF GRADE CODE
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 29: COLOR & LEAF GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES
Fiber Competition, Cotton Incorporated

## Slide 30: INFORMATION ON THE WEB
For updates on U.S. Cotton Fiber Quality:
https://www.cottoninc.com/cotton-production/quality/cotton-crop-quality/
Fiber Competition, Cotton Incorporated