## Slide 1: U.S. UPLAND COTTON QUALITY
2020-21 CROP
FINAL

## Slide 2
YIELD TREND U.S. UPLAND
POUNDS/ACRE
YEAR

## Slide 3: MICRONAIRE

## Slide 4: MICRONAIRE TREND U.S. UPLAND
MICRONAIRE
YEAR
Chart: 
| 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020
 | 4.5341 | 4.5166 | 4.3948 | 4.4808 | 4.4163 | 4.428 | 4.0534 | 4.3922 | 4.4726 | 4.2678

## Slide 5: MICRONAIRE DISTRIBUTION U.S. UPLAND
MICRONAIRE
PERCENT OF SAMPLES

## Slide 6: AVERAGE MICRONAIRE
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2018 | 4.5228 | 4.2766 | 4.7328 | 4.65 | 4.6861 | 4.6646 | 4.1606 | 4.0709 | 3.9896 | 4.4737
2019 | 4.626 | 4.5342 | 4.559 | 4.4576 | 4.6472 | 4.3762 | 4.3024 | 4.3386 | 4.4784 | 4.497
2020 | 4.2523 | 4.4472 | 4.5137 | 4.388 | 4.5871 | 4.3195 | 3.9156 | 3.7694 | 4.0721 | 4.4616
CLASSING OFFICE
MICRONAIRE

## Slide 7: AVERAGE MICRONAIRE
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2018 | 4.4527 | 4.3823 | 4.2476 | 4.3753 | 4.5653 | 4.6526 | 4.7639 | 4.6772 | 4.7955 | 4.6177 | 4.688 | 4.6646 | 4.1606 | 4.0709 | 3.9896 | 4.2751 | 3.8391 | 4.1166 | 4.5645 | 4.3412
2019 | 4.5744 | 4.3787 | 4.5429 | 4.5732 | 4.6358 | 4.6822 | 4.5311 | 4.5905 | 4.5673 | 4.5008 | 4.5194 | 4.3762 | 4.3024 | 4.3386 | 4.4784 | 4.4255 | 3.8376 | 4.2705 | 4.5738 | 4.3832
2020 | 4.2899 | 4.4171 | 4.4634 | 4.2866 | 4.2396 | 4.237 | 4.4633 | 4.6332 | 4.558 | 4.3618 | 4.3045 | 4.3195 | 3.9156 | 3.7694 | 4.0721 | 4.0432 | 3.2988 | 4.2613 | 4.5715 | 4.2592
MICRONAIRE
LOCATION
Far West
Southwest
Mid South
Southeast

## Slide 8: STRENGTH

## Slide 9: STRENGTH TREND U.S. UPLAND
GRAMS/TEX
YEAR
Chart: 
| 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020
 | 29.9544 | 29.8665 | 30.2238 | 30.0579 | 30.3444 | 30.339 | 29.9075 | 29.9014 | 30.6086 | 30.6073

## Slide 10: STRENGTH DISTRIBUTION U.S. UPLAND
GRAMS/TEX
PERCENT OF SAMPLES

## Slide 11: AVERAGE STRENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2018 | 29.5093 | 28.818 | 30.0064 | 29.6638 | 30.0975 | 29.442 | 29.6592 | 30.8283 | 30.1434 | 32.254
2019 | 30.9404 | 29.9476 | 30.9497 | 30.2843 | 30.9317 | 30.9105 | 31.3206 | 30.5614 | 30.3553 | 32.1563
2020 | 29.9431 | 29.9226 | 31.3938 | 31.0616 | 30.885 | 30.8824 | 30.651 | 30.3982 | 30.2969 | 31.9502
CLASSING OFFICE
GRAMS/TEX

## Slide 12: AVERAGE STRENGTH
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2018 | 28.4143 | 28.9673 | 28.8376 | 28.8445 | 29.9508 | 29.1309 | 29.4359 | 29.9437 | 30.361 | 29.8575 | 29.933 | 29.442 | 29.6592 | 30.8283 | 30.1434 | 30.0465 | 28.9709 | 30.2878 | 31.3608 | 34.461
2019 | 30.3183 | 29.6891 | 29.9602 | 30.2334 | 31.1794 | 31.1524 | 29.9487 | 30.826 | 31.1124 | 30.6961 | 30.405 | 30.9105 | 31.3206 | 30.5614 | 30.3553 | 32.1053 | 30.7114 | 30.5838 | 31.567 | 33.5317
2020 | 30.2173 | 30.2719 | 29.8333 | 29.6554 | 30.1255 | 29.7212 | 30.6277 | 30.9529 | 31.6114 | 31.2533 | 31.2192 | 30.8824 | 30.651 | 30.3982 | 30.2969 | 31.148 | 29.5278 | 30.1427 | 31.6451 | 33.1215
GRAMS/TEX
LOCATION
Far West
Southwest
Mid South
Southeast

## Slide 13: LENGTH

## Slide 14: LENGTH TREND U.S. UPLAND
32’s OF AN INCH
YEAR
Chart: 
| 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020
 | 35.4794 | 35.7038 | 35.8506 | 35.6512 | 35.8955 | 36.2879 | 36.4464 | 36.5288 | 36.4708 | 37.0888

## Slide 15: LENGTH DISTRIBUTION U.S. UPLAND
PERCENT OF SAMPLES
32’S OF AN INCH

## Slide 16: AVERAGE LENGTH
Chart: 
| Fl, SC | Ma, GA | Ra, LA | Me, TN | Du, AR | CC, TX | Ab, TX | Lu, TX | La, TX | Vi, CA
2018 | 36.3598 | 36.5712 | 36.7563 | 37.1027 | 37.3985 | 35.7832 | 35.9032 | 36.0374 | 35.8037 | 37.5799
2019 | 36.713 | 36.3846 | 37.8199 | 37.1082 | 37.7079 | 36.0202 | 35.9764 | 35.1943 | 34.5652 | 37.2815
2020 | 37.5337 | 37.0632 | 38.1446 | 38.0697 | 38.3969 | 36.5824 | 36.2288 | 35.7633 | 35.1055 | 37.2076
CLASSING OFFICE
32’S OF AN INCH

## Slide 17: AVERAGE LENGTH
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2018 | 37.2224 | 36.6889 | 36.5154 | 36.595 | 36.359 | 35.894 | 36.3993 | 37.2444 | 37.1656 | 37.5572 | 37.4628 | 35.7832 | 35.9032 | 36.0374 | 35.8037 | 36.0639 | 35.7689 | 37.8898 | 37.321 | 38.0432
2019 | 37.2685 | 36.449 | 36.4051 | 36.4906 | 36.6958 | 37.2404 | 36.4328 | 37.6019 | 38.0571 | 37.5328 | 37.3339 | 36.0202 | 35.9764 | 35.1943 | 34.5652 | 36.4795 | 36.0008 | 37.5445 | 37.1415 | 37.5201
2020 | 37.6472 | 37.3196 | 37.0221 | 37.5257 | 37.4158 | 38.091 | 37.3545 | 38.2687 | 38.5824 | 38.4899 | 38.381 | 36.5824 | 36.2288 | 35.7633 | 35.1055 | 36.9726 | 35.2281 | 36.7763 | 37.0704 | 37.6
32’S OF AN INCH
LOCATION
Far West
Southwest
Mid South
Southeast

## Slide 18: LENGTH UNIFORMITY INDEX

## Slide 19: LUI TREND U.S. UPLAND
LUI PERCENT
YEAR

## Slide 20: LENGTH UNIFORMITY DISTRIBUTION U.S. UPLAND
LUI PERCENT
PERCENT OF SAMPLES

## Slide 21: AVERAGE LENGTH UNIFORMITY
CLASSING OFFICE
LUI PERCENT

## Slide 22: AVERAGE LENGTH UNIFORMITY
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2018 | 80.607 | 80.9826 | 81.0416 | 80.3674 | 80.8065 | 80.5992 | 81.5868 | 81.1315 | 80.9935 | 81.7979 | 82.3018 | 80.8814 | 80.3183 | 80.9362 | 80.455 | 80.4893 | 80.7241 | 82.1805 | 81.3773 | 82.4928
2019 | 81.8195 | 81.083 | 81.6059 | 81.1731 | 81.5952 | 82.0495 | 81.554 | 81.4546 | 81.8997 | 81.893 | 82.2601 | 80.9411 | 80.621 | 80.4744 | 79.7171 | 80.9906 | 80.6592 | 82.0285 | 81.3793 | 82.0071
2020 | 81.2428 | 81.2686 | 81.3984 | 81.2029 | 81.5421 | 81.8046 | 81.8545 | 81.6433 | 82.0839 | 81.9346 | 82.2449 | 81.2157 | 80.2844 | 80.247 | 79.7801 | 80.6432 | 79.8232 | 81.105 | 81.0901 | 81.5605
LUI PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION

## Slide 23: COLOR & LEAF

## Slide 24: COLOR GRADE TREND U.S. UPLAND
YEAR
PERCENT COLOR GRADE

## Slide 25: COLOR GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES

## Slide 26: PERCENT WHITE GRADES
CLASSING OFFICE
PERCENT

## Slide 27: PERCENT WHITE GRADES
Chart: 
| FL | AL | GA | SC | NC | VA | TN | MS | LA | AR | MO | CC TX | Ab TX | Lu TX | La TX | OK | KS | NM | AZ | CA
2018 | 76.5216 | 75.1406 | 85.5126 | 83.3688 | 84.0623 | 86.4691 | 62.3746 | 88.0404 | 76.5933 | 81.3771 | 85.5848 | 62.3683 | 77.8602 | 88.8251 | 81.1451 | 86.0197 | 61.652 | 98.962 | 89.7444 | 94.3629
2019 | 93.7013 | 90.4334 | 92.316 | 94.0111 | 97.0115 | 97.9766 | 96.1957 | 96.8925 | 94.3187 | 98.4973 | 99.1681 | 77.2677 | 76.2923 | 44.5747 | 57.9683 | 86.8183 | 56.0068 | 86.3086 | 93.2913 | 96.1231
2020 | 91.2221 | 89.1388 | 89.0266 | 94.0844 | 94.6281 | 96.3533 | 98.247 | 96.8114 | 91.4729 | 98.9305 | 99.358 | 84.3697 | 81.0551 | 86.9178 | 85.4841 | 83.6544 | 70.2175 | 99.0125 | 98.2362 | 98.7223
PERCENT
Far West
Southwest
Mid South
Southeast
LOCATION

## Slide 28: LEAF GRADE DISTRIBUTION U.S. UPLAND
LEAF GRADE CODE
PERCENT OF SAMPLES

## Slide 29: COLOR & LEAF GRADE DISTRIBUTION U.S. UPLAND
COLOR GRADE CODE
PERCENT OF SAMPLES

## Slide 30: INFORMATION ON THE WEB
http://www.cottoninc.com/fiber/quality/Crop-Quality-Reports/